Filter Lenses for Protection against Radiant Energy

| Operations | Electrodes Size 1/32 Inches | Arc Current | Minimum Protective Shade |
| --- | --- | --- | --- |
| Shielded metal arc welding | less than 3 | less than 60 | 7 |
|  | 3-5 | 60-160 | 8 |
|  | 5-8 | 60-250 | 10 |
|  | more than 8 | 250-550 | 11 |
| Gas metal arc welding Flux cored arc welding |  | less than 60 | 7 |
|  |  | 60-160 | 10 |
|  |  | 60-250 | 10 |
|  |  | 250-500 | 10 |
| Gas Tungsten arc welding |  | less than 50 | 8 |
|  |  | 50-150 | 8 |
|  |  | 150-500 | 10 |
| Air Carbon | Light | less than 500 | 10 |
| Air cutting | Heavy | 500-1000 | 11 |
| Plasma arc welding |  | less than 20 | 6 |
|  |  | 20-100 | 8 |
|  |  | 100-400 | 10 |
|  |  | 400-800 | 11 |
| Plasma arc cutting | light* | less than 300 | 8 |
|  | medium** | 300-400 | 9 |
|  | heavy** | 400-800 | 10 |
| Torch Brazing |  |  | 3 |
| Torch soldering |  |  | 2 |
| Carbon arc welding |  |  | 14 |

*  As a rule of thumb start with a shade that is too dark to see the weld zone then switch a lighter shade which gives sufficient view of the weld zone without going below the minimum shade allowed.  In oxyfuel gas welding or cutting where the torch produces a high yellow light, use a filter lens that absorbs the yellow (sodium line) in the visual light of the (spectrum) operation.

** These values apply where the actual arc is clearly seen.  Experience has shown that lighter filters may be used when the arc is hidden by the work piece.

Filter Lenses for Protection against Radiant Energy

| Operations | Plate thickness-inches | Plate thickness-mm | Minimum* Protective Shade |
| --- | --- | --- | --- |
| Gas Welding | Under 1/8 | Under 3.2 | 4 |
| Light |  |  |  |
| Medium | 1/8 to 1/2 | 3.2 to 12.7 | 5 |
| Heavy | Over 1/2 | Over 12.7 | 6 |
| Oxygen cutting | Under 1 | Under 25 | 3 |
| Light |  |  |  |
| Medium | 1 to 6 | 25 to 150 | 4 |
| Heavy | Over 6 | Over 150 | 5 |
| Carbon arc welding |  |  | 14 |

*  As a rule of thumb start with a shade that is too dark to see the weld zone then switch a lighter shade which gives sufficient view of the weld zone without going below the minimum shade allowed.  In oxyfuel gas welding or cutting where the torch produces a high yellow light, use a filter lens that absorbs the yellow (sodium line) in the visual light of the (spectrum) operation.

# Text boxes

Table 1 continues on the next page.